## Slide 1: SDM Pouring Guide
Model T
Ver. 0.4

## Slide 2: Overview
Print fingers
Pour joint material
Pour pad material
Cure (24-48 hours)
Cut away frame material

## Slide 3: Materials List
PMC-780 Urethane [link]
  Two-part rubber compound
  PMC-790 too stiff for general use cases
  Demold time: 48 hours
Vytaflex-20/30 Urethane [link]
  Two part urethane rubber
  Demold time: 16 hours

## Slide 4: Pre-Pour Preparation
Seal bottom of printed fingers
Do not pour directly on top of 3D printer support material
  Fingerpad urethane can leak through support material
Heat duct tape works best for sealing

## Slide 5: Vacuum, De-Gassing
- vacuum setup
Material de-gassed prior to pour
Urethane will rise 2-3x initial level during de-gassing
  ~ 30 seconds
  Remove urethane from chamber after initial rise in level subsides

## Slide 6: Fingerpad Pouring
1A : 1B part ratio
Viscosity low relative to that of flexure joint material
  De-gassing not necessary
  Susceptible to leaking – pour more than necessary if possible

## Slide 7: Flexure Pouring
2A : 1B part ratio
High viscosity
  Joint will work without de-gassing
  More consistent behavior if vacuum and de-gassing is used
Pour more material than necessary
  Excess urethane can be removed later

## Slide 8: Frame Removal
ABS frame ~0.7-1.0 mm thick
  Bandsaw or file used to cut out frame elements
  Compliance of joints/pads minimizes damage if cut is excessive
  Can partially cut and then “snap” frame elements apart
File or belt sander used to smooth, file-down excess ABS or urethane material