## Slide 1
Dieless Deposition Manufacturing
Instructions
Last updated: November 11, 2013

## Slide 2: Introduction/Summary
Approach #1: Breakaway Mold Walls
Print finger frames via 3D printer
Seal/tape finger frames
Prepare rubber urethane mixtures
Pour joint flexure urethanes
Pour finger pad urethanes
Wait for urethanes to cure (24-48 hours)
Cut away sacrificial walls
Step-by-step video also available at: www.youtube.com/watch?v=dEJJMax7hs0
Approach #2: Multi-Part Molds
Print finger and mold parts
Assemble snap-together mold
Prepare rubber urethane mixtures
Pour joint flexure urethanes
Pour finger pad urethanes
Wait for urethanes to cure
Disassemble mold walls slowly (tabs are included on mold pieces to aid in disassembly)
Clean-up leftover urethane material
Step-by-step video also available at:
http://www.youtube.com/watch?v=iqePcD0VAmc
1

## Slide 3: Process Comparison
2
Breakaway Mold Walls | Multi-Part Molds
Minimizes material that needs to be printed | Requires full set of mold pieces for each finger
Requires band-saw post-processing | Has no sacrificial 3D-printed pieces
Requires ability to print thin (~0.7mm) sacrificial walls | Mold components have minimum 3mm feature size, which might make it easier for lower-end printers
Cannot be re-used, must re-print every time | Outer mold components are reusable
Single piece print, no inter-part dependencies | Mold components must fit together properly
Molds need to be sealed with tape | Mold pieces snap into place, no adhesives necessary
Possible urethane leakage due to tape not adhering properly to mold | Possible urethane leakage due to mold components not fitting tightly together
Smaller sacrificial pieces minimizes potential damage to flexures/pads | Care should be taken during mold disassembly to avoid pulling out finger pads

## Slide 4: Selected Urethanes
3
Finger Joints:
PMC-780 Urethane [link]
  Two-part rubber compound
  PMC-790 too stiff for general use cases
  Demold time: 48 hours
Alternatives:
  Task 16 [link]
Finger Pads:
Vytaflex-20/30 Urethane [link]
  Two part urethane rubber
  PMC-780 and other Vytaflex options can act as suitable replacements
  Demold time: 16 hours
Alternatives:
  Econ 80 [link]
Commercial rubber urethanes are mixed just like two-part epoxy
Mix according to ratios in instructions, either by volume or mass
  Mass scale will need 0.1g precision due to small quantity that is mixed
Approximately ~5-8g of total urethane is needed per finger for each component
  This will vary depending on your finger parameters and leakage

## Slide 5: Sealing/Taping
4
Remove all support material prior to pouring
DO NOT pour on top of support material
  Urethanes will leak through support material
Use tape to seal bottom of finger molds as shown above
  Most adhesives will suffice
  Some leakage is expected, not critical
  Try to ensure that tape remains affixed to bottom of finger molds
  Heating duct tape and masking tape are preferred

## Slide 6: Mold Assembly/Disassembly
5
Mold components should fit snugly together and snap into the bottom plate
  Printing errors between matching parts will increase urethane leakage
Easiest to assemble all parts except for bottom plate first, then snap into the bottom place
Easiest to disassemble by removing bottom plate first, then pealing away the side walls
  Wall in contact with urethanes may be difficult to remove
  Release agents like mold-release or wax may be applied to walls in contact with urethane to aid in removal

## Slide 7: Pouring
6
Pour from as high and with as thin a stream as possible
Pour more than necessary
  Excess material can be cut off and removed later
  Additional urethane may need to be poured if urethane leaks
Less viscous urethanes have higher chances of leakage
  Users can wait ~10 min for urethanes to become more viscous and easier to pour if desired
  However, waiting too long before pouring may not give urethane enough time to set in the cavities, resulting in excess bubbles and poorly-formed flexures
Tips/suggestions for pouring also available via the urethane distributor at www.smooth-on.com

## Slide 8: Degassing (Optional)
7
Why Degas?
More evenly distributed bubble/imperfection formation
Higher density
Higher stiffness
Higher degree of manufacturing repeatability
Degas
No Degassing
Solutions:
Low vacuum in dessicator (see figure to the left)
  Leave mixed urethane in vacuum for < 2 min
  User should observe the urethane rise/fall
Consider alternative urethanes that set more quickly
  Alternative urethanes from those listed in this guide have not been tested in OpenHand projects

## Slide 9: Wall Removal
8
ABS frame ~0.7-1.0 mm thick
  Bandsaw or file used to cut out frame elements
  Compliance of joints/pads minimizes damage if cut is excessive
  Can partially cut and then “snap” frame elements apart
File, blade, or belt sander can be used to smooth, file-down excess ABS or urethane material
Be careful to avoid accidentally cutting into the flexure
  Tears in flexure material will degrade performance and robustness
Be careful to preserve tendon-entry holes during removal of walls from finger pads